## Slide 1
Fluoropolymer Incineration: Evidence for the Lack of PFAS Emissions
Philip H Taylor1, Hans-Joachim Gehrmann2, Krasmir Aleksandrov2, Sven Herremans3, Meg Michell4, David Blye4, Deepak Kapoor5, Priyank Dalal5, Pyrianga Gunasekar5, Andrei Bologa2, Philipp Bergdolt2, Vanessa Nuredin2, Dieter Stapf2, M. Schlipf
1
5
4
3
2
H-J Gehrmann, et al., Mineralization of Fluoropolymers from Combustion in a Pilot Plant under Representative European Municipal and Hazardous Waste Combustor Conditions, Chemosphere, 365, 143403, 2024.https://doi.org/10.1016/j.chemosphere.2024.143403.

## Slide 2: Introduction
PFAS
Per- and polyFluoroAlkyl Substances
> 13000 human-made chemicals
oil and water-resistant
https://www.spektrum.de/wissen/pfas-umweltgifte-fuer-die-ewigkeit/1724648, download 19.03.2024
Source: https://echa.europa.eu/de/hot-topics/perfluoroalkyl-chemicals-pfas
universal PFAS restriction proposal
ECHA receives more than 5600 comments
ECHA
high cholesterol
certain cancers
reduced vaccine response
pregnancy induced hypertension
Health effects

## Slide 3
Incineration of fluoropolymers:
PFAS analysis along the flue gas pathway
A pilot scale trial at operational conditions similar to municipal and industrial incineration plants that typically burn products containing fluoropolymers was conducted to assess the potential generation of any statistically significant uncontrolled emissions of Per- and Polyfluoroalkyl Substances at levels that might present a risk

## Slide 4: Project partners
Research partner Institute for Technical Chemistry (ITC) at Karlsruhe Institute of Technology (KIT)
Sampling partner SGS Institut Fresenius GmbH, Industries & Environment
Laboratory partner SGS Belgium NV, Institute for Applied Chromatography
Feed sampling Pro-K, Fluoropolymer Processing and Downstream User Association, Germany
Incineration Advisor P Taylor & Associates, LLC, USA
Data quality review Environmental Standards Inc., USA
Observer UBA, Umweltbundesamt (German Federal Environment Agency)

## Slide 5: Test facility BRENDA / sampling locations
2.5 MWth

## Slide 6: Flow regime in a kiln versus a grate
Source: Lecture „Thermal Waste Treatment“, IFK Stuttgart
Cross current flow
Co-current flow
& fuel
& fuel

## Slide 7: Experimental setup
mass flow = 320 g/h
Basis of fluoropolymer feed mixture:
Feed mixture comprises four largest volume fluoropolymers - PTFE, PVDF, PFA, FKM. Together these represent 80% of commercial fluoropolymer production
Pro-K supplied fluoropolymer samples of major applications that were grinded and mixed
Setting | Test Conditions |  | 
 | Background combustion with oil, natural gas and wood chips | Combustion with oil, natural gas, wood chips and FP | Background combustion with oil, natural gas and wood chips
 | Start-up of pilot plant |  | 
1 | RUN 1 | RUN 2 | RUN 3
 | Change of temperature in post-combustion chamber |  | 
2 | RUN 4 | RUN 5 | RUN 6
 | Shut down of pilot plant |  | 

## Slide 8: Main operational parameters, setting 1 and 2
- 200 kW, shift thermal power to the PCC
+ 260 kW, total power ≈ constant
Increase of temperature by reduction of
stoichiometric air/fuel ratio
Increase of rotation speed to avoid slagging
Setting S1:
conc. CO = 1,35 [mg/m³] = 4.5 ppm
Setting S2:
conc. CO = 1,64 [mg/m³] = 6.58 ppm

## Slide 9: Sampling and Analysis
SGS sampling train
Ultrahigh-Performance Liquid Chromatography coupled to tandem Mass Spectrometer (UPLC-MS/MS) for targeted long-chain PFAS and Trifluoroacetic Acid (TFA)
Gas Chromatography coupled to Mass Spectrometry (GC-MS) for volatile fluorocarbons
Tunable diode laser (TDL) for Hydrogen Fluoride at boiler exit
Ion Chromatography for fluoride ion at the stack

## Slide 11: Testing methodology
27 samples analyzed per setting
3 samples were collected and analyzed at each sampling point per setting (triplicate sampling)
PFAS analyzed at Pre-run, Run and Post-run conditions
Scrubber water and ash samples analyzed for target PFAS content
Blank media and solutions were analyzed for their respective parameters
Blanks from sample train were analyzed at relevant sample locations

## Slide 12: Statistical evaluation, example for PFBA
Measured value PFBA < LOQ  c = 0
Value RUN 1*
Median (50. Percentile)
Measured value PFBA < LOQ  c = ½ LOQ
Median (50. Percentile)
Value RUN 1 + ½ LOQ
[ng/mN3 dry]
* from quartz filter, in the condensate and in the three impingers all values are < LOQ
[ng/mN3 dry]
Source: Compendium of water sampling, measurement and analysis 2024, https://reflabos.vito.be/2024/WAC_IV_A_025.pdf, only in Dutch available, on page 14, first line: If a sum of PFAS needs to be made, the "lower bound principle" needs to be applied.

## Slide 13: HF measurement at boiler exit (Tunable Diode Laser)

## Slide 14: Fluorine mass balance

## Slide 15: Fluorine mass emission rates from PFAS

## Slide 16: Fluorine mass emission rates from PFAS

## Slide 17: Results
Targeted PFAS analysis: Statistical analysis of the PFAS emissions measurements indicated that PFOA was the only PFAS that was detected above the LOQ (0.20 ng/m3) in the stack gas sample in the 1095°C FP combustion test. This result is not considered definitive, however, as PFOA was also detected in 8 other combustion test samples where the FP was not fed (at levels ranging from 0.04 -1.19 ng/m3).
PFAS analysis of wastewater and ash residue: Statistical analysis of the wastewater and ash residue samples indicated that PFBS and PFOS were detected above the LOQ. These results are questionable given that the FP fed did not contain measurable amounts of sulfur. The source of the PFBS and PFOS may be memory effects or the presence of traces of sulfur in the wood chips fed to support the combustion process.
Trifluoroacetic acid: TFA was not detected at a reporting limit of 50 ng/m3.
GC-MS analysis for short chain fluorocarbons: C1-C3 fluorocarbons were non detected in the flue gases at LOQs ranging from 5 - 40 mg/m3.
Fluorine Recovery: Fluorine recoveries ranged from 70 to 80% using Tunable Diode Laser detection of HF - provides strong evidence for mineralization of the fluoropolymer feed mixture.

## Slide 18: Conclusions
Fluoropolymers in incinerators operated according to the EU Directive regulations are converted to inorganic fluorides and carbon dioxide.
Statistical analysis of the combustion runs demonstrated that PFOA was the only detectable PFAS in the gas stream. Seven other PFAS were detected in the FP combustion runs but were considered outliers in the statistical analysis.
Inorganic fluorides were detected as hydrogen fluoride (between 70 to 80 wt. % F recovery). Lower F recoveries at 1095°C suggest that F feed rate may not have been well controlled.
The decrease in PCC temperature from 1095°C to 860°C did not show an increase in PFAS, TFA, or C1-C3 emissions.
Fluoropolymers pose low risk to human health and the environment at their end of life when incinerated.

## Slide 19: Acknowledgements
This study was funded by Gujarat Fluorochemicals GmbH
For further information, contact:
Deepak Kapoor: dkapoor@gfl.co.in
Phil Taylor: Taylorphd6397@gmail.com
Hans-Joachim Gehrmann: Hans-Joachim.Gehrmann@kit.edu

## Slide 20: Questions?
for your attention!

## Slide 21: Experimental setup
mass flow = 320 g/h
Basis of fluoropolymer feed mixture:
Feed mixture comprises of four largest volume fluoropolymers - PTFE, PVDF, PFA, FKM. Together these represent 80% of commercial fluoropolymer production
Pro-K supplied fluoropolymer samples of major applications that were grinded and mixed

## Slide 22: Measurement and Analytics OTM 45
03.03.2025
X
modification by SGS
Rinsing solution: 5% ammonium hydroxide in methanol
Impinger bottles are analyzed individually
Blank values are measured
Setup and methodology are modified according to the experience of the sampler